S P E C I F I C A T I O N S

AMMONIUM FLUORIDE ACS

CAS No:				12125-01-8

Formula:				NH4F

F.W.:					37.04

Description:				Colorless or White deliquescent solid

Assay:					98% minimum

Insoluble Matter:			0.005% maximum

Residue on Ignition:		0.01%  maximum

Chloride (Cl):			0.001% maximum

Sulfate:				0.005% maximum

Heavy metals (as Pb):		5ppm

Iron (Fe):				5ppm

Effective: 07/02/12