S P E C I F I C A T I O N S

AMMONIUM THIOCYANATE ACS

Synonyms: 					Ammonium sulfocyanide; Ammonium rhodanide; thiocyanic acid, ammonium salt, ammonium sulfocyanate

CAS No:					1762-95-4

Chemical Formula:				NH4SCN

Formula Weight:				76.12

Description:					Colorless to White crystalline powder

Assay:						> 98.0%

Appearance:					Conforms to structure

Insoluble Matter:				≤ 0.005%

Residue after Ignition:			≤ 0.025%

Chloride  (Cl):				≤ 0.005%

Sulfate  (SO4): 				≤ 0.005%

Heavy Metals  (as Pb):			≤ 5 ppm

Iron  (Fe):					≤ 3 ppm

pH (of a 5% solution at 25˚C):		4.5 – 6.0

Iodine – consuming substances:		0.004 mg/g

Effective: 10/18/2011