S P E C I F I C A T I ON S

POTASSIUM PHOSPHATE, TRIBASIC ANHYDROUS ACS

Synonyms:				Tripotassium phosphate anhydrous

Tripotassium orthophosphate anhydrous

Chemical Formula:			K3 PO4

Formula Weight:			212.27

CAS No.:				7778-53-2

Appearance:				White granular-powder

Assay:	 				98%  minimum

Dibasic potassium phosphate	1%  maximum

Excess alkali (as KOH):		1%  maximum

Insoluble matter:			0.01%  maximum

Chloride (Cl):			0.005%  maximum

Heavy metals (as Pb):		0.002%  maximum

Iron (Fe):				0.001%  maximum

Sulfate (SO4):			0.005%  maximum

Sodium (Na):			0.1%  maximum

Effective: 09/01/13