S P E C I F I C A T I O N S

SILVER METALLIC POWDER

Synonyms				None

CAS No.				7440-22-4

Description				Grey, odorless powder

Identification A,B,C		To pass tests

Silver Content			≥99.0%

Solubility				Insoluble in water.

Loss on Drying			1% maximum

Particle Size:				D50  3,5 < 15µm

D10 ≤ 3µm

D90 ≤ 50µm

BET (surface area):			3-5 m2 / g

Total Aerobic Mesophilic Count	< 1.000 UFC/g

Total Mold & Yeast Count 	<1.000 UFC/g

E.Coli				No Growth

S.aureus			No Growth

P.aeruginosa			No Growth

C.albicans			No Growth

Effective: 11/21/14