S P E C I F I C A T I O N S

SILVER ZEOLITE

Synonyms				None known

CAS No.				130328-18-6

Formula:				Mx/n [(A1O2)x (SiO2)y].w H2O

Appearance				White powder

Mean Particle Size			D50   3-5µm

Humidity				< 10%

Silver content			2.3% - 2.7%

Solubility				Insoluble in Water

Total Aerobic Mesophilic count:		< 1.000 UFC/g

Total Mold & Yeast count:			<1.000 UFC/g

E.Coli					No Growth

S.aureus				No Growth

P.aeruginosa				No Growth

C.albicans				No Growth

Effective Date: 11/01/2018