S P E C I F I C A T I O N S

SODIUM  FLUORIDE ACS

Synonyms:						Alcoa Sodium Fluoride

CAS No.:						7681-49-4

Chemical Formula:					FNa

Formula Weight:					41.99 g/mol

Appearance:						Fine, white or slightly yellow powder

Assay (Titrimetry):					> 99.0% (NaF)

Titrable Acid (meq/g):				≤0.03

Titrable Base (meq/g):				≤0.01

Insoluble Matter					<0.02%

Chloride(Cl)						< 50 ppm

Heavy metals(as Pb)				< 30 ppm

Iron(Fe)						< 30 ppm

Sulfate(SO4)						< 300 ppm

Potassium (K) 					< 200 ppm

Effective: 11/29/12